# CS Hyde Company

    - FAX: 800-441-8063

# 1351 North Milwaukee Avenue

# Lake Villa, IL  60046				PRODUCT INFORMATION

## Product Description:

The LT Series lacing tapes are well suited for most applications requiring lacing tape (flat braid) or tie cord (round braid) to operate at extreme temperatures and in chemically aggressive environments.  Our lacing tapes will not burn or support flame, they also will not rot or support fungus.  In addition, our braided products are PTFE impregnated prior to braiding, thus increasing flexibility and knot strength versus other competitive products that are braided first, them PTFE coated.

Performance & Application Information:

| Features | Benefits |
| --- | --- |
| High Temperature Resistance | Chemical Resistance |
| High Strength | Minimal Buildup of Contaminants |
| Uniform PTFE coating | Excellent Knot Strength |
| Each Yard Individually Coated | Excellent Thermal Shock Resistance |
| Excellent Flexibility | Will Not Burn or Support Flame |

### TYPICAL PROPERTIES

| Product | - - - - - - - 779-SERIES - - - - - - - - |
| --- | --- |
| Number | LT-779-18 | LT-779-15 | LT-779-11 | LT-779-13 | LT-779-7 |
| Coating Type | PTFE, Unsintered |
| Braid Type | Flat |
| Yield (yds/lb) | 220 | 325 | 520 | 430 | 1025 |
| Thickness (in.) | .018 | .015 | .011 | .013 | .007 |
| Width (in.) | 1/8 | 7/64 | 3/32 | 5/64 | 3/64 |
| Diameter (in.) | N/A |
| Tensile (lb/min) | 150 | 125 | 90 | 60 | 40 |

| Product | - - - - 761-Series - - - - |
| --- | --- |
| Number | LT-761-.047 | LT-761-.034 | LT-761-.027 |
| Coating Type | - - - PTFE, Unsintered - - - |
| Braid Type | - - Round - - |
| Yield (yds/lb) | 360 | 540 | 1150 |
| Thickness (in.) | N/A |
| Width (in.) | N/A |
| Diameter (in.) | .047 | .034 | .027 |
| Tensile (lb/min) | 80 | 75 | 50 |

# Text boxes

LT-__  Series

Braided PTFE Coated E-Glass Lacing Tapes and Tie Cords